SRBF F2

Information Technology Solutions

ABOUT THIS PRODUCT

LPF-2 Grade material is manufactured from medium weaved, cotton Fabric. The material of this grade has a superior machiningg and punching properties and better resistance of chemicals. Recommended for small parts

APPLICATIONS

• Rigid
• Strong in both directions
• Easily machined

FEATURES AND BENEFITS

• Rigid
• Strong in both directions
• Easily machined

23 Ullswater Crescent

Coulsdon

Surrey

CR5 2UY

TEL: +44(0) 20 8668 1481

WEB: www.croylek.com

EMAIL: sales@croylek.co.uk

MATERIAL DATA

| Grade | LRF- 2 (F2) |
| --- | --- |
| Thickness | 0.4mm-150.0mm |
| Size | Standard sizes are 2440 x 1220 / 1220 x 1220mm |
| Specifications Met | BS:2572: GRADE F2/EN-60893-3-4-PFCC203 DIN7735-GRADE HGW 2083 DIN:7735 GRADE HGW:2082.5 |

TECHNICAL TABLE

| Properties | Units | Average | Values as per test results IS:2036-1995 |
| --- | --- | --- | --- |
| Mechanical: |  |  |  |
| Tensile Strength | Kgf/cm2 | 700 | -- |
| Flexural strength/Cross |  |  |  |
| Breaking Strength | Kgf/cm2 | 1200 | 1100 Min. |
| Shear Strength | Kgf/cm2 | 745 | 650 Min. |
| Impact Strength (Edgewise) | KJ/m2 | 9 | 7 Min. |
| Specific Gravity |  | 1.35 | ---------- |
| Electrical |  |  |  |
| Electrical Strength in oil at 90°C |  |  |  |
| *Flat wide 1.6mm thickness | Kv/mm | 1.5 | 0.72 Min. |
| *Edgewise 3.2mm thickness | Kv | 4 | 1.0 Min |
| Insulation Resistance | Meg Ohms | 10 | 0.5 Min |
| After immersion in water. For 24 hrs at 20°C |  |  |  |

| Water Absorption |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| *Thickness | mm | 0.8 | 3.0 | 12.0 | 25.0 |
| *Maximum Value | mg | 201 | 245 | 324 | 420 |
| Average Test Results | Mg | 68 | 89 | 112 | 154 |