| MAterial - technical card |  | PN: | 119 867 500 |  |
| --- | --- | --- | --- | --- |
| Designation of product: | insulating tapes |  |  |  |
| Product number (PN): | 119 867 500. |  |  |  |
| Finishing: | without finishing = 0 |  |  |  |
| Structure and technology charakteristics |  |  |  |  |
| Material composition / % /: | 99 fibreglass, 1 polyester |  |  |  |
| Produced widths, tolerance / mm /: | 50,0 |  |  | +1,0;- 2,5 |
| Thickness / mm /: | 0,23 ± 0,03 |  |  |  |
| Weight, cca / g/m /: | 12,1 |  |  |  |
| DELIVERY – usual finish |  |  |  |  |
| Length of winding / m /: | 400, rolls |  |  |  |

23 Ullswater Crescent

Coulsdon

Surrey  CR5 2UY

Tel : 020 8668 1481

Fax : 020 8660 0750

email : gary@croylek.co.uk

web : www.croylek.co.uk

A company registered in England No. 824514

VAT No. 830 3683 40